#### TABLE OF CONTENTS

I. 	Foreword	3

II. 	General description	3

III 	Chips	4

IV 	Radial leaded capacitors	6

V 	“CNC” Series	9

VI 	“SC” and “SV” Series	11

VII 	“TB” Series	15

VII 	Dielectric characteristics	16

V 	Electrical characteristics	18

VII 	Termination types	19

VIII 	Special products	19

IX 	How to order	20

X	Packaging	21

# I. Foreword

These capacitors have been developed in response to demand from switched mode power supply (S.M.P.S.) and DC-DC converters manufacturers. They are particularly suitable for filtering, smoothing and decoupling purpose in Hi-Rel equipments. The capacitors utilize advanced ceramic technology to achieve Hi-Rel long operating life and small size. They are designed for hybrid assemblies and low profile printed circuit applications.

Customized assemblies may be achieved with standard bare chip sizes mentioned in the following chapters.

# II. General description

The capacitors here mentioned concern the voltage equal or higher than 50V, in bare chips or leaded devices. Two dielectrics are proposed in X7R Class: the “X” series and the “T” series. Each of them has it own characteristics in between the “X7R” Class limitations.

Bare chips (SMD):

Leaded devices on assemblies (examples):

# III Chips

III-1 Features

The SMD or chips components are the basis capacitors of all the leaded assemblies. Generally not used as chips especially for the sizes above 2229 for soldering reasons (cf the soldering recommendation), the tables hereunder are given for the capacitance range and the thickness of these basis capacitors.

III-2 Capacitance range

| Cr | Cr | 2229 | 3033 | 3740 | 5440 |
| --- | --- | --- | --- | --- | --- |
| Code | (µF) | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V |
| 104 | 0.10 |  |  |  |  | 1.8 |  | 3.0 | 2.3 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 124 | 0.12 |  |  |  |  | 1.8 |  | 3.0 | 2.3 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 154 | 0.15 |  |  |  |  | 2.0 |  |  | 2.3 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 184 | 0.18 |  |  |  |  | 2.0 |  |  | 2.6 |  |  |  |  |  |  | 3.2 | 2.6 |  |  |  |  |  |  | 3.0 | 2.6 |  |  |  |  |  |  |  |  |
| 224 | 0.22 |  |  |  |  | 2.5 |  |  | 2.8 |  |  |  |  |  |  | 3.2 | 2.6 |  |  |  |  |  |  | 3.0 | 2.6 |  |  |  |  |  |  | 3.0 | 2.7 |
| 274 | 0.27 |  |  |  |  | 2.5 | 2.3 |  | 3.1 |  |  |  |  | 2.0 |  | 3.5 | 2.6 |  |  |  |  |  |  | 3.0 | 2.6 |  |  |  |  |  |  | 3.0 | 2.7 |
| 334 | 0.33 | 1.8 |  | 1.8 |  | 2.5 | 2.3 |  |  |  |  |  |  | 2.0 |  |  | 2.8 |  |  |  |  | 2.0 |  | 3.3 | 2.6 |  |  |  |  | 2.5 |  | 3.5 | 2.7 |
| 394 | 0.39 | 1.8 |  | 1.8 |  | 2.5 | 2.3 |  |  |  |  |  |  | 2.0 |  |  | 3.1 |  |  |  |  | 2.0 |  | 3.5 | 2.6 |  |  |  |  | 2.5 |  | 3.5 | 2.7 |
| 474 | 0.47 | 1.8 |  | 1.8 |  |  | 2.3 |  |  |  |  |  |  | 2.0 | 2.3 |  | 3.5 |  |  |  |  | 2.0 |  | 4.0 | 2.6 |  |  |  |  | 2.5 |  | 3.5 | 2.7 |
| 564 | 0.56 | 2.0 |  | 2.0 |  |  | 2.5 |  |  |  |  |  |  | 2.5 | 2.3 |  |  |  |  |  |  | 2.0 |  |  | 2.9 | 2.0 |  | 2.0 |  | 2.5 | 2.6 | 3.8 | 2.7 |
| 684 | 0.68 | 2.0 | 2.3 | 2.0 | 2.3 |  | 2.8 |  |  | 2.0 |  | 2.0 |  | 3.0 | 2.3 |  |  |  |  |  |  | 2.5 |  |  | 3.4 | 2.0 |  | 2.0 |  | 2.5 | 2.6 | 4.0 | 2.7 |
| 824 | 0.82 | 2.0 | 2.3 | 2.0 | 2.3 |  |  |  |  | 2.0 |  | 2.0 |  | 3.5 | 2.4 |  |  |  |  |  |  | 2.5 | 2.3 |  | 3.8 | 2.0 |  | 2.0 |  | 3.0 | 2.6 | 4.2 | 2.7 |
| 105 | 1.0 | 2.2 | 2.3 | 2.2 | 2.3 |  |  |  |  | 2.5 |  | 2.5 |  |  | 2.6 |  |  | 2.0 |  | 2.0 |  | 3.0 | 2.3 |  |  | 2.0 |  | 2.0 |  | 3.0 | 2.6 |  | 2.7 |
| 125 | 1.2 | 2.5 | 2.3 | 2.5 | 2.3 |  |  |  |  | 2.5 |  | 2.5 |  |  | 2.9 |  |  | 2.0 |  | 2.0 |  | 3,5 | 2.3 |  |  | 2.0 |  | 2.0 |  | 3.5 | 2.6 |  | 3.3 |
| 155 | 1.5 | 2.5 | 2.3 | 3.0 | 2.3 |  |  |  |  | 2.8 | 2.3 | 2.8 | 2.3 |  | 3.4 |  |  | 2.0 | 2.3 | 2.0 | 2.3 | 4.0 | 2.6 |  |  | 2.0 |  | 2.0 |  | 3.5 | 2.6 |  | 3.9 |
| 185 | 1.8 |  | 2.3 |  | 2.3 |  |  |  |  | 2.8 | 2.3 | 2.8 | 2.3 |  |  |  |  | 2.5 | 2.3 | 2.5 | 2.3 |  | 2.8 |  |  | 2.0 |  | 2.0 |  | 4.0 | 2.6 |  |  |
| 225 | 2.2 |  | 2.6 |  | 2.6 |  |  |  |  | 2.8 | 2.3 | 2.8 | 2.3 |  |  |  |  | 2.5 | 2.3 | 2.5 | 2.3 |  | 3.2 |  |  | 2.5 | 2.6 | 2.5 | 2.6 | 4.0 | 2.6 |  |  |
| 275 | 2.7 |  | 2.9 |  | 2.9 |  |  |  |  | 3.3 | 2.4 | 3.3 | 2.4 |  |  |  |  | 2.8 | 2.3 | 2.8 | 2.3 |  | 3.6 |  |  | 2.5 | 2.6 | 2.5 | 2.6 |  | 2.6 |  |  |
| 335 | 3.3 |  |  |  |  |  |  |  |  | 3.8 | 2.5 | 3.8 | 2.5 |  |  |  |  | 2.8 | 2.3 | 2.8 | 2.3 |  |  |  |  | 3.0 | 2.6 | 3.0 | 2.6 |  | 3.3 |  |  |
| 395 | 3.9 |  |  |  |  |  |  |  |  |  | 2.8 |  | 2.8 |  |  |  |  | 3.3 | 2.3 | 3.3 | 2.3 |  |  |  |  | 3.0 | 2.6 | 3.0 | 2.6 |  | 3.7 |  |  |
| 475 | 4.7 |  |  |  |  |  |  |  |  |  | 3.1 |  | 3.1 |  |  |  |  | 3.5 | 2.3 | 3.5 | 2.3 |  |  |  |  | 3.0 | 2.6 | 3.0 | 2.6 |  |  |  |  |
| 565 | 5.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.6 |  | 2.6 |  |  |  |  | 3.5 | 2.6 | 3.5 | 2.6 |  |  |  |  |
| 685 | 6.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 3.0 |  | 3.0 |  |  |  |  | 3.5 | 2.6 | 3.5 | 2.6 |  |  |  |  |
| 825 | 8.2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 3.6 |  | 3.6 |  |  |  |  | 3.8 | 2.6 | 3.8 | 2.6 |  |  |  |  |
| 106 | 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.8 |  | 2.8 |  |  |  |  |
| 126 | 12 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 3.2 |  | 3.2 |  |  |  |  |
| 156 | 15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 186 | 18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 226 | 22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 276 | 27 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

The thickness (Tmax in mm) is indicated in the cells.

| Cr | Cr | 5550 | 6560 | 6080/8060 | 45107 |
| --- | --- | --- | --- | --- | --- |
| Code | (µF) | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V |
| 104 | 0.10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 124 | 0.12 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 154 | 0.15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 184 | 0.18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 224 | 0.22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 274 | 0.27 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 334 | 0.33 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 394 | 0.39 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 474 | 0.47 |  |  |  |  |  |  | 3.0 | 2.6 |  |  |  |  |  |  | 2.5 | 2.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 564 | 0.56 |  |  |  |  |  |  | 3.0 | 2.6 |  |  |  |  | 2.0 |  | 2.5 | 2.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 684 | 0.68 |  |  |  |  |  |  | 3.0 | 2.6 |  |  |  |  | 2.0 |  | 2.5 | 2.6 |  |  |  |  |  |  | 3.0 | 2.6 |  |  |  |  |  |  | 3.5 | 3.1 |
| 824 | 0.82 |  |  |  |  | 3.0 |  | 3.5 | 2.6 |  |  |  |  | 2.0 |  | 3.0 | 2.6 |  |  |  |  |  |  | 3.0 | 2.6 |  |  |  |  | 3.0 | 3.0 | 3.5 | 3.1 |
| 105 | 1.0 |  |  |  |  | 3.0 |  | 4.2 | 2.8 | 2.0 |  | 2.0 |  | 2.0 | 2.6 | 3.0 | 2.6 |  |  |  |  |  |  | 3.0 | 2.6 | 3.0 |  | 3.0 |  | 3.0 | 3.0 | 3.8 | 3.1 |
| 125 | 1.2 |  |  |  |  | 3.0 | 2.6 |  | 3.3 | 2.0 |  | 2.0 |  | 2.0 | 2.6 | 3.5 | 2.6 |  |  |  |  |  |  | 3.5 | 2.6 | 3.0 |  | 3.0 |  | 3.0 | 3.0 | 3.8 | 3.1 |
| 155 | 1.5 |  |  |  |  | 3.0 | 2.6 |  | 3.6 | 2.0 |  | 2.0 |  | 2.5 | 2.6 | 4.0 | 3.0 |  |  |  |  | 3.0 |  | 4.0 | 2.6 | 3.0 | 3.0 | 3.0 | 3.0 | 3.0 | 3.0 |  | 3.1 |
| 185 | 1.8 | 2.5 |  | 2.5 |  | 3.0 | 2.6 |  | 4.1 | 2.0 |  | 2.0 |  | 2.5 | 2.6 | 4.5 | 3.0 |  |  |  |  | 3.0 |  | 4.5 | 2.6 | 3.0 | 3.0 | 3.0 | 3.0 | 3.0 | 3.0 |  | 3.1 |
| 225 | 2.2 | 2.5 |  | 2.5 |  | 3.0 | 2.6 |  |  | 2.0 |  | 2.0 |  | 2.5 | 2.6 |  | 3.3 |  |  |  |  | 3.0 | 2.6 |  | 2.6 | 3.0 | 3.0 | 3.0 | 3.0 | 3.5 | 3.0 |  | 3.1 |
| 275 | 2.7 | 2.5 |  | 2.5 |  | 3.5 | 2.6 |  |  | 2.0 | 2.6 | 2.0 | 2.6 | 3.0 | 2.6 |  | 3.8 |  |  |  |  | 3.0 | 2.6 |  | 3.3 | 3.0 | 3.0 | 3.0 | 3.0 | 3.8 | 3.0 |  | 3.1 |
| 335 | 3.3 | 2.5 | 2.6 | 2.5 | 2.6 | 4.0 | 2.8 |  |  | 2.0 | 2.6 | 2.0 | 2.6 | 3.0 | 2.6 |  | 4.3 |  |  |  |  | 3.0 | 2.6 |  | 3.9 | 3.0 | 3.0 | 3.0 | 3.0 | 4.0 | 3.0 |  |  |
| 395 | 3.9 | 2.5 | 2.6 | 2.5 | 2.6 |  | 3.1 |  |  | 2.0 | 2.6 | 2.0 | 2.6 | 3.5 | 2.6 |  |  | 3.0 |  | 3.0 |  | 3.5 | 2.6 |  | 4.4 | 3.0 | 3.0 | 3.0 | 3.0 |  | 3.0 |  |  |
| 475 | 4.7 | 3.0 | 2.6 | 3.0 | 2.6 |  | 3.5 |  |  | 2.0 | 2.6 | 2.0 | 2.6 | 4.0 | 2.6 |  |  | 3.0 |  | 3.0 |  | 4.0 | 2.6 |  |  | 3.0 | 3.0 | 3.0 | 3.0 |  | 3.0 |  |  |
| 565 | 5.6 | 3.0 | 2.6 | 3.0 | 2.6 |  |  |  |  | 2.5 | 2.6 | 2.5 | 2.6 |  | 2.9 |  |  | 3.0 |  | 3.0 |  |  | 2.6 |  |  | 3.0 | 3.0 | 3.0 | 3.0 |  | 3.0 |  |  |
| 685 | 6.8 | 3.0 | 2.6 | 3.0 | 2.6 |  |  |  |  | 2.5 | 2.6 | 2.5 | 2.6 |  | 3.3 |  |  | 3.0 | 2.6 | 3.0 | 2.6 |  | 3.0 |  |  | 3.0 | 3.0 | 3.0 | 3.0 |  |  |  |  |
| 825 | 8.2 | 3.5 | 2.6 | 3.5 | 2.6 |  |  |  |  | 3.0 | 2.6 | 3.0 | 2.6 |  | 3.8 |  |  | 3.0 | 2.6 | 3.0 | 2.6 |  | 3.6 |  |  | 3.0 | 3.0 | 3.0 | 3.0 |  |  |  |  |
| 106 | 10 | 3.8 | 2.6 | 3.8 | 2.6 |  |  |  |  | 3.0 | 2.6 | 3.0 | 2.6 |  |  |  |  | 3.5 | 2.6 | 3.5 | 2.6 |  |  |  |  | 3.5 | 3.0 | 3.5 | 3.0 |  |  |  |  |
| 126 | 12 |  | 2.8 |  | 2.8 |  |  |  |  | 3.5 | 2.6 | 3.5 | 2.6 |  |  |  |  | 3.5 | 2.6 | 3.5 | 2.6 |  |  |  |  | 3.5 | 3.0 | 3.5 | 3.0 |  |  |  |  |
| 156 | 15 |  | 3.2 |  | 3.2 |  |  |  |  | 4.0 | 2.6 | 4.0 | 2.6 |  |  |  |  | 3.5 | 2.6 | 3.5 | 2.6 |  |  |  |  |  | 3.0 |  | 3.0 |  |  |  |  |
| 186 | 18 |  |  |  |  |  |  |  |  |  | 2.6 |  | 2.6 |  |  |  |  | 3.5 | 2.6 | 3.5 | 2.6 |  |  |  |  |  | 3.0 |  | 3.0 |  |  |  |  |
| 226 | 22 |  |  |  |  |  |  |  |  |  | 3.0 |  | 3.0 |  |  |  |  |  | 2.8 |  | 2.8 |  |  |  |  |  | 3.0 |  | 3.0 |  |  |  |  |
| 276 | 27 |  |  |  |  |  |  |  |  |  | 3.6 |  | 3.6 |  |  |  |  |  | 3.3 |  | 3.3 |  |  |  |  |  | 3.3 |  | 3.3 |  |  |  |  |

The thickness (Tmax in mm) is indicated in the cells.

III-3 Dimensions

All dimensions in mm

| Size | L | Tol | W | Tol | EB | EB |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | (min) | (max) |
| 2229 | 5.7 | 0.4 | 7.4 | 0.4 | 0.25 | 1.4 |
| 3033 | 7.4 | 0.5 | 8.0 | 0.5 | 0.5 | 2.0 |
| 3740 | 9.6 | 0.5 | 9.8 | 0.5 | 0.5 | 2.0 |
| 5440 | 13.7 | 0.5 | 10.2 | 0.5 | 0.5 | 2.0 |
| 5550 | 13.7 | 0.5 | 12.3 | 0.5 | 0.5 | 2.0 |
| 6080 | 15 | 0.8 | 19.8 | 0.8 | 0.5 | 2.0 |
| 6560 | 17.2 | 0.8 | 15.5 | 0.8 | 0.5 | 2.0 |
| 8060 | 19.8 | 0.8 | 14.9 | 0.8 | 0.5 | 2.0 |
| 45107 | 11.0 | 0.5 | 27.5 max | 0.5 | 2.0 |

The thickness is indicated in the capacitance range tables

# IV Radial leaded capacitors

IV-1 Features

Connected by 2 wires, these components have only one basis chips. This 2 wires termination makes the parts perfectly suitable to any design capable to withstand severe environmental conditions (chocks, bumps, vibrations…). An epoxy coating is applied to protect the parts, the parts are marked.

IV-2 Capacitance range

| Cr | Cr | R2229 | R3033 | R3740 | R5440 |
| --- | --- | --- | --- | --- | --- |
| Code | (µF) | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V |
| 104 | 0.10 |  |  |  |  | 3.1 |  | 4.3 | 3.5 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 124 | 0.12 |  |  |  |  | 3.1 |  | 4.3 | 3.5 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 154 | 0.15 |  |  |  |  | 3.3 |  | 4.5 | 3.7 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 184 | 0.18 |  |  |  |  | 3.3 |  |  | 3.9 |  |  |  |  |  |  | 4.5 | 3.9 |  |  |  |  |  |  | 4.3 | 3.9 |  |  |  |  |  |  |  |  |
| 224 | 0.22 |  |  |  |  | 3.8 |  |  | 4.2 |  |  |  |  |  |  | 4.5 | 3.9 |  |  |  |  |  |  | 4.3 | 3.9 |  |  |  |  |  |  | 4.3 | 4.0 |
| 274 | 0.27 |  |  |  |  | 3.8 | 3.5 |  | 4.6 |  |  |  |  | 3.3 |  | 4.8 | 3.9 |  |  |  |  |  |  | 4.3 | 3.9 |  |  |  |  |  |  | 4.3 | 4.0 |
| 334 | 0.33 | 3.1 |  | 3.1 |  | 3.8 | 3.5 |  |  |  |  |  |  | 3.3 |  |  | 4.1 |  |  |  |  | 3.3 |  | 4.6 | 3.9 |  |  |  |  | 3.8 |  | 4.8 | 4.0 |
| 394 | 0.39 | 3.1 |  | 3.1 |  | 4.3 | 3.5 |  |  |  |  |  |  | 3.3 |  |  | 4.4 |  |  |  |  | 3.3 |  | 4.8 | 3.9 |  |  |  |  | 3.8 |  | 4.8 | 4.0 |
| 474 | 0.47 | 3.1 |  | 3.1 |  |  | 3.7 |  |  |  |  |  |  | 3.3 | 3.6 |  | 4.8 |  |  |  |  | 3.3 |  | 5.3 | 3.9 |  |  |  |  | 3.8 |  | 4.8 | 4.0 |
| 564 | 0.56 | 3.3 |  | 3.3 |  |  | 3.9 |  |  |  |  |  |  | 3.8 | 3.6 |  |  |  |  |  |  | 3.3 |  |  | 4.2 | 3.3 |  | 3.3 |  | 3.8 | 3.9 | 5.1 | 4.0 |
| 684 | 0.68 | 3.3 | 3.5 | 3.3 | 3.5 |  |  |  |  | 3.3 |  | 3.3 |  | 4.3 | 3.6 |  |  |  |  |  |  | 3.8 |  |  | 4.7 | 3.3 |  | 3.3 |  | 3.8 | 3.9 | 5.3 | 4.0 |
| 824 | 0.82 | 3.3 | 3.5 | 3.3 | 3.5 |  |  |  |  | 3.3 |  | 3.3 |  | 4.8 | 3.7 |  |  |  |  |  |  | 3.8 | 3.6 |  | 5.1 | 3.3 |  | 3.3 |  | 4.3 | 3.9 | 5.5 | 4.0 |
| 105 | 1.0 | 3.5 | 3.5 | 3.5 | 3.5 |  |  |  |  | 3.8 |  | 3.8 |  |  | 3.9 |  |  | 3.3 |  | 3.3 |  | 4.3 | 3.6 |  |  | 3.3 |  | 3.3 |  | 4.3 | 3.9 |  | 4.0 |
| 125 | 1.2 | 3.8 | 3.5 | 3.8 | 3.5 |  |  |  |  | 3.8 |  | 3.8 |  |  | 4.2 |  |  | 3.3 |  | 3.3 |  | 4.8 | 3.6 |  |  | 3.3 |  | 3.3 |  | 4.8 | 3.9 |  | 4.6 |
| 155 | 1.5 | 3.8 | 3.5 | 4.3 | 3.5 |  |  |  |  | 4.1 | 3.6 | 4.3 | 3.6 |  | 4.7 |  |  | 3.3 | 3.6 | 3.3 | 3.6 | 5.3 | 3.9 |  |  | 3.3 |  | 3.3 |  | 4.8 | 3.9 |  | 5.2 |
| 185 | 1.8 | 4.3 | 3.5 | 4.3 | 3.5 |  |  |  |  | 4.1 | 3.6 | 4.3 | 3.6 |  |  |  |  | 3.8 | 3.6 | 3.8 | 3.6 |  | 4.1 |  |  | 3.3 |  | 3.3 |  | 5.3 | 3.9 |  |  |
| 225 | 2.2 |  | 4.0 |  | 4.0 |  |  |  |  | 4.1 | 3.6 | 4.3 | 3.6 |  |  |  |  | 3.8 | 3.6 | 3.8 | 3.6 |  | 4.5 |  |  | 3,8 | 3.9 | 3.8 | 3.9 | 5.3 | 3.9 |  |  |
| 275 | 2.7 |  | 4.3 |  | 4.3 |  |  |  |  | 4.6 | 3.7 | 4.6 | 3.7 |  |  |  |  | 4.1 | 3.6 | 4.1 | 3.6 |  | 4.9 |  |  | 3.8 | 3.9 | 3.8 | 3.9 |  | 3.9 |  |  |
| 335 | 3.3 |  |  |  |  |  |  |  |  | 5.1 | 3.8 | 5.1 | 3.8 |  |  |  |  | 4.1 | 3.6 | 4.1 | 3.6 |  |  |  |  | 4.3 | 3.9 | 4.3 | 3.9 |  | 4.6 |  |  |
| 395 | 3.9 |  |  |  |  |  |  |  |  |  | 4.1 |  | 4.1 |  |  |  |  | 4.6 | 3.6 | 4.6 | 3.6 |  |  |  |  | 4.3 | 3.9 | 4.3 | 3.9 |  | 5.0 |  |  |
| 475 | 4.7 |  |  |  |  |  |  |  |  |  | 4.4 |  | 4.4 |  |  |  |  | 4.8 | 3.6 | 4.8 | 3.6 |  |  |  |  | 4.3 | 3.9 | 4.3 | 3.9 |  |  |  |  |
| 565 | 5.6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 3.9 |  | 3.9 |  |  |  |  | 4.8 | 3.9 | 4.8 | 3.9 |  |  |  |  |
| 685 | 6.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 4.3 |  | 4.3 |  |  |  |  | 4.8 | 3.9 | 4.8 | 3.9 |  |  |  |  |
| 825 | 8.2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 4.9 |  | 4.9 |  |  |  |  | 5.1 | 3.9 |  | 3.9 |  |  |  |  |
| 106 | 10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 4.1 |  | 4.1 |  |  |  |  |
| 126 | 12 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 4.5 |  | 4.5 |  |  |  |  |
| 156 | 15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 186 | 18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 226 | 22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 276 | 27 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

The thickness (Tmax in mm) is indicated in the cells.

|  | Cr | Cr | R5550 | R6560 | R6080/R8060 |
| --- | --- | --- | --- | --- | --- |
|  | Code | (µF) | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V |
|  | 104 | 0.10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 124 | 0.12 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 154 | 0.15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 184 | 0.18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 224 | 0.22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 274 | 0.27 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  |  |  |
|  | 334 | 0.33 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  |  |  |
|  | 394 | 0.39 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  |  |  |
|  | 474 | 0.47 |  |  |  |  |  |  | 4.3 | 3.9 |  |  |  |  |  |  | 3.8 | 3.9 |  |  |  |  |  |  |  |  |
|  | 564 | 0.56 |  |  |  |  |  |  | 4.3 | 3.9 |  |  |  |  | 3.3 |  | 3.8 | 3.9 |  |  |  |  |  |  |  |  |
|  | 684 | 0.68 |  |  |  |  |  |  | 4.3 | 3.9 |  |  |  |  | 3.3 |  | 3.8 | 3.9 |  |  |  |  |  |  | 4.3 | 3.9 |
|  | 824 | 0.82 |  |  |  |  | 4.3 |  | 4.3 | 3.9 |  |  |  |  | 3.3 |  | 4.3 | 3.9 |  |  |  |  |  |  | 4.3 | 3.9 |
|  | 105 | 1.0 |  |  |  |  | 4.3 |  | 5.5 | 4.1 | 3.3 |  | 3.3 |  | 3.3 | 3.9 | 4.3 | 3.9 |  |  |  |  |  |  | 4.3 | 3.9 |
|  | 125 | 1.2 |  |  |  |  | 4.3 | 3.9 |  | 4.6 | 3.3 |  | 3.3 |  | 3.3 | 3.9 | 4.8 | 3.9 |  |  |  |  |  |  | 4.8 | 3.9 |
|  | 155 | 1.5 |  |  |  |  | 4.3 | 3.9 |  | 4.9 | 3.3 |  | 3.3 |  | 3.8 | 3.9 | 5.3 | 4.3 |  |  |  |  | 4.3 |  | 5.3 | 3.9 |
|  | 185 | 1.8 | 3.8 |  | 3.8 |  | 4.3 | 3.9 |  | 5.4 | 3.3 |  | 3.3 |  | 3.8 | 3.9 | 5.8 | 4.3 |  |  |  |  | 4.3 |  | 5.8 | 3.9 |
|  | 225 | 2.2 | 3.8 |  | 3.8 |  | 4.3 | 3.9 |  |  | 3.3 |  | 3.3 |  | 3.8 | 3.9 |  | 4.6 |  |  |  |  | 4.3 | 3.9 |  | 3.9 |
|  | 275 | 2.7 | 3.8 |  | 3.8 |  | 4.8 | 3.9 |  |  | 3.3 | 3.9 | 3.3 | 3.9 | 4.3 | 3.9 |  | 5.1 |  |  |  |  | 4.3 | 3.9 |  | 4.6 |
|  | 335 | 3.3 | 3.8 | 3.9 | 3.8 | 3.9 | 5.3 | 4.1 |  |  | 3.3 | 3.9 | 3.3 | 3.9 | 4.3 | 3.9 |  | 5.6 |  |  |  |  | 4.3 | 3.9 |  | 5.2 |
|  | 395 | 3.9 | 3.8 | 3.9 | 3.8 | 3.9 |  | 4.4 |  |  | 3.3 | 3.9 | 3.3 | 3.9 | 4.8 | 3.9 |  |  | 4.3 |  | 4.3 |  | 4.8 | 3.9 |  | 5.7 |
|  | 475 | 4.7 | 4.3 | 3.9 | 4.3 | 3.9 |  | 4.8 |  |  | 3.3 | 3.9 | 3.3 | 3.9 | 5.3 | 3.9 |  |  | 4.3 |  | 4.3 |  | 5.3 | 3.9 |  |  |
|  | 565 | 5.6 | 4.3 | 3.9 | 4.3 | 3.9 |  |  |  |  | 3.8 | 3.9 | 3.8 | 3.9 |  | 2.9 |  |  | 4.3 |  | 4.3 |  |  | 3.9 |  |  |
|  | 685 | 6.8 | 4.3 | 3.9 | 4.3 | 3.9 |  |  |  |  | 3.8 | 3.9 | 3.8 | 3.9 |  | 4.6 |  |  | 4.3 | 3.9 | 4.3 | 3.9 |  | 4.3 |  |  |
|  | 825 | 8.2 | 4.8 | 3.9 | 4.8 | 3.9 |  |  |  |  | 4.3 | 3.9 | 4.3 | 3.9 |  | 5.1 |  |  | 4.3 | 3.9 | 4,3 | 3.9 |  | 4.9 |  |  |
|  | 106 | 10 | 5.1 | 3.9 | 5.1 | 3.9 |  |  |  |  | 4.3 | 3.9 | 4.3 | 3.9 |  |  |  |  | 4.8 | 3.9 | 4.8 | 3.9 |  |  |  |  |
|  | 126 | 12 |  | 4.1 |  | 4.1 |  |  |  |  | 4.8 | 3.9 | 4.8 | 3.9 |  |  |  |  | 4.8 | 3.9 | 4.8 | 3.9 |  |  |  |  |
|  | 156 | 15 |  | 4.5 |  | 4.5 |  |  |  |  | 5.3 | 3.9 | 5.3 | 3.9 |  |  |  |  | 4.8 | 3.9 | 4.8 | 3.9 |  |  |  |  |
|  | 186 | 18 |  |  |  |  |  |  |  |  |  | 3.9 |  | 3.9 |  |  |  |  | 7.5 | 3.9 | 7.5 | 3.9 |  |  |  |  |
|  | 226 | 22 |  |  |  |  |  |  |  |  |  | 4.3 |  | 4.3 |  |  |  |  |  | 4.1 |  | 4.1 |  |  |  |  |
|  | 276 | 27 |  |  |  |  |  |  |  |  |  | 4.9 |  | 4.9 |  |  |  |  |  | 4.6 |  | 4.6 |  |  |  |  |

The thickness (Tmax in mm) is indicated in the cells.

IV-3 Dimensions

All dimensions in mm

| Size | W max | H max | LS ±0.5 | D ±10% |
| --- | --- | --- | --- | --- |
| 2229 | 7.6 | 9.8 | 5.08 | 0.5 |
| 3033 | 10.2 | 10.5 | 5.08 | 0.5 |
| 3740 | 12.7 | 12.3 | 10.2 | 0.6 |
| 5440 | 17.2 | 12.7 | 15.2 | 0.9 |
| 5550 | 17.2 | 14.8 | 15.2 | 0.9 |
| 6080 | 18.8 | 22.6 | 15.2 | 0.9 |
| 6560 | 20.3 | 18.3 | 17.8 | 0.9 |
| 8060 | 23.6 | 17.7 | 20.3 | 0.9 |

The thickness is indicated in the capacitance range tables

IV-4 Marking

| Size | Marking codes | Example |
| --- | --- | --- |
| ≤ 2229 | Cap Code + Tolerance Code Rated voltage value |  |
| > 2229 | « TA » logo Cap Code + Tolerance Code Rated voltage value |  |

.

# V “CNC” Series

V-1 Features

These products are derived from the standard R5440 and R6560 basis chips. This family has the same performance than the radial lead components family. Other capacitances versus rated voltages is completing the range of the radial lead components family Also connected with 2 wires, the coating and the marking are applied.. The “X” dielectric only is available at the moment.

IV-2 Capacitance range

|  |  | CHIPS | RADIAL LEADED DEVICES |
| --- | --- | --- | --- |
| Cr | Cr | CNC5440 | CNC6560 | CNC5440 | CNC6560 |
| Code | (µF) | 63V | 100V | 250V | 400V | 63V | 100V | 250V | 400V | 63V | 100V | 250V | 400V | 63V | 100V | 250V | 400V |
| 104 | 0.10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 124 | 0.12 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 154 | 0.15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 184 | 0.18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 224 | 0.22 |  |  |  | 2.5 |  |  |  |  |  |  |  | 3.8 |  |  |  |  |
| 274 | 0.27 |  |  |  | 2.5 |  |  |  | 2.0 |  |  |  | 3.8 |  |  |  | 3.3 |
| 334 | 0.33 |  |  | 2.5 | 2.5 |  |  |  | 2.0 |  |  | 3.8 | 3.8 |  |  |  | 3.3 |
| 394 | 0.39 |  |  | 2.5 | 3.0 |  |  |  | 2.0 |  |  | 3.8 | 4.3 |  |  |  | 3.3 |
| 474 | 0.47 |  |  | 2.5 | 3.0 |  |  |  | 2.0 |  |  | 3.8 | 4.3 |  |  |  | 3.3 |
| 564 | 0.56 |  | 2.0 | 2.5 | 3.0 |  |  | 2.0 | 2.0 |  | 3.3 | 3.8 | 4.3 |  |  | 3.3 | 3.3 |
| 684 | 0.68 |  | 2.0 | 3.0 | 3.5 |  |  | 2.0 | 2.5 |  | 3.3 | 4.3 | 4.8 |  |  | 3.3 | 3.8 |
| 824 | 0.82 |  | 2.0 | 3.0 | 4.0 |  |  | 2.0 | 3.0 |  | 3.3 | 4.3 | 5.3 |  |  | 3.3 | 4.3 |
| 105 | 1.0 |  | 2.0 | 3.0 | 4.4 |  | 2.0 | 2.0 | 3.0 |  | 3.3 | 4.3 | 5.7 |  | 3.3 | 3.3 | 4.3 |
| 125 | 1.2 |  | 2.0 | 3.5 |  |  | 2.0 | 2.0 | 3.5 |  | 3.3 | 4.8 |  |  | 3.3 | 3.3 | 4.8 |
| 155 | 1.5 | 2.0 | 2.0 | 3.5 |  | 2.0 | 2.0 | 2.5 | 4.0 | 3.3 | 3.3 | 4.8 |  | 3.3 | 3.3 | 3.8 | 5.3 |
| 185 | 1.8 | 2.5 | 2.5 | 4.0 |  | 2.0 | 2.0 | 2.5 | 5.0 | 3.3 | 3.8 | 5.3 |  | 3.3 | 3.3 | 3.8 | 6.3 |
| 225 | 2.2 | 2.5 | 2.5 | 4.0 |  | 2.0 | 2.0 | 2.5 |  | 3.8 | 3.8 | 5.3 |  | 3.3 | 3.3 | 3.8 |  |
| 275 | 2.7 | 2.5 | 2.5 |  |  | 2.0 | 2.0 | 3.0 |  | 3.8 | 3.8 |  |  | 3.3 | 3.3 | 4.3 |  |
| 335 | 3.3 | 3.0 | 3.0 |  |  | 2.0 | 2.0 | 3.0 |  | 4.3 | 4.3 |  |  | 3.3 | 3.3 | 4.3 |  |
| 395 | 3.9 | 3.0 | 3.0 |  |  | 2.0 | 2.0 | 3.5 |  | 4.3 | 4.3 |  |  | 3.3 | 3.3 | 4.8 |  |
| 475 | 4.7 | 3.0 | 3.0 |  |  | 2.0 | 2.0 |  |  | 4.3 | 4.3 |  |  | 3.3 | 3.3 |  |  |
| 565 | 5.6 | 3.5 | 3.5 |  |  | 2.5 | 2.5 |  |  | 4.8 | 4.8 |  |  | 3.8 | 3.8 |  |  |
| 685 | 6.8 | 3.5 | 3.5 |  |  | 2.5 | 2.5 |  |  | 4.8 | 4.8 |  |  | 3.8 | 3.8 |  |  |
| 825 | 8.2 | 3.8 | 3.8 |  |  | 3.0 | 3.0 |  |  | 5.1 | 5.1 |  |  | 4.3 | 4.3 |  |  |
| 106 | 10 |  |  |  |  | 3.0 | 3.0 |  |  |  |  |  |  | 4.3 | 4.3 |  |  |
| 126 | 12 |  |  |  |  | 3.5 | 3.5 |  |  |  |  |  |  | 4.8 | 4.8 |  |  |
| 156 | 15 |  |  |  |  | 4.0 | 4.0 |  |  |  |  |  |  | 5.3 | 5.3 |  |  |

The thickness (Tmax in mm) is indicated in the cells.

V-3 Dimensions

All dimensions in mm

| Size | L | Tol | W | Tol | EB | EB |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | (min) | (max) |
| CNC5440 | 13.7 | 0.5 | 10.2 | 0.5 | 0.5 | 2.0 |
| CNC6560 | 17.2 | 0.8 | 15.5 | 0.8 | 0.5 | 2.0 |

| Size | W max | H max | LS ±0.5 | D ±10% |
| --- | --- | --- | --- | --- |
| CNC5440 | 17.2 | 12.7 | 15.24 | 0.9 |
| CNC6560 | 20.3 | 18.3 | 17.8 | 0.9 |

All dimensions in mm

Note: products in 100V can also be order under “R5440” or “R6560” case codes since there is no technical differences between both designations

V-4 Marking

| Size | Marking codes | Example |
| --- | --- | --- |
| CNC5440 CNC6560 | « TA » logo Cap Code + Tolerance Code Rated voltage value |  |

# VI “SC” and “SV” Series

VI-1 Features

The « SV » Series looks like the radial 2 wires components Series except the assemblies are made with 2 to 4 basis chips. This allows to extend the 2 wires family.

The “SC” Series offer 4 wires (W4), Dual In Line (DIL) or ribbons terminations making them perfectly suitable to any design (ceramic substrate, epoxy board…) capable to withstand severe environmental conditions (shocks, bumps, vibrations…) as the “SV” Series.

VI-2 Capacitance range

| Cr | Cr | SC00 (2229) | SC01/SV01 (3033) | SC02/SV02 (3740) | SC03/SV03 (5440) |
| --- | --- | --- | --- | --- | --- |
| Code | (µF) | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V | 50V | 100V | 200V 250 V | 500V 400V |
| 104 | 0.10 |  |  |  |  | 2.0 |  | 3.2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 124 | 0.12 |  |  |  |  | 2.0 |  | 3.2 |  |  |  |  |  |  |  | 2.7 | 2.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 154 | 0.15 |  |  |  |  | 2.2 |  | 6.4 |  |  |  |  |  |  |  | 2.7 | 2.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 184 | 0.18 |  |  |  |  | 2.2 |  | 6.4 |  |  |  |  |  |  |  | 3.4 | 2.8 |  |  |  |  |  |  | 3.2 | 2.8 |  |  |  |  |  |  |  |  |
| 224 | 0.22 |  |  |  |  | 2.7 |  | 6.4 |  |  |  |  |  |  |  | 3.4 | 2.8 |  |  |  |  |  |  | 3.2 | 2.8 |  |  |  |  |  |  | 2.7 | 2.9 |
| 274 | 0.27 |  |  |  |  | 2.7 |  | 9.6 |  |  |  |  |  | 2.2 |  | 5.4 | 2.8 |  |  |  |  |  |  | 3.2 | 2.8 |  |  |  |  |  |  | 2.7 | 2.9 |
| 334 | 0.33 | 2.2 |  | 2.2 |  | 4.4 |  | 9.6 |  |  |  |  |  | 2.2 |  | 6.1 | 3 |  |  |  |  | 2.2 |  | 3.5 | 2.8 |  |  |  |  | 2.7 |  | 2.7 | 2.9 |
| 394 | 0.39 | 2.2 |  | 2.2 |  | 4.4 |  | 13 |  |  |  |  |  | 2.2 |  | 6.1 | 3.3 |  |  |  |  | 2.2 |  | 3.7 | 2.8 |  |  |  |  | 2.7 |  | 3.2 | 2.9 |
| 474 | 0.47 | 2.2 |  | 2.2 |  | 5.4 |  | 12.8 |  |  |  |  |  | 2.2 | 2.5 | 6.9 | 3.7 |  |  |  |  | 2.2 |  | 6.4 | 2.8 |  |  |  |  | 2.7 |  | 3.2 | 2.9 |
| 564 | 0.56 | 2.2 |  | 2.2 |  | 5.4 |  | 13.6 |  |  |  |  |  | 2.7 | 2.5 | 10.5 | 5.6 |  |  |  |  | 2.2 |  | 6.7 | 3.1 | 2.2 |  | 2.2 |  | 2.7 | 2.8 | 3.2 | 2.9 |
| 684 | 0.68 | 2.2 |  | 2.2 |  | 8.1 |  |  |  | 2.2 |  | 2.2 |  | 4.4 | 2.5 | 10.5 | 6.3 |  |  |  |  | 2.7 |  | 7.0 | 3.6 | 2.2 |  | 2.2 |  | 3.2 | 2.8 | 3.7 | 2.9 |
| 824 | 0.82 | 2.2 |  | 2.2 |  | 8.1 |  |  |  | 2.2 |  | 2.2 |  | 4.4 | 2.6 | 13.9 | 6.6 |  |  |  |  | 2.7 | 2.5 | 9.9 | 4.0 | 2.2 |  | 2.2 |  | 3.2 | 2.8 | 4.2 | 2.9 |
| 105 | 1.0 | 2.4 |  | 2.4 |  | 10.8 |  |  |  | 2.7 |  | 2.7 |  | 4.4 | 2.8 | 14.8 | 7.4 | 2.2 |  | 2.2 |  | 3.2 | 2.5 | 10.3 | 5.9 | 2.2 |  | 2.2 |  | 3.2 | 2.8 | 4.6 | 2.9 |
| 125 | 1.2 | 2.7 |  | 2.7 |  | 10.8 |  |  |  | 2.7 |  | 2.7 |  | 5.4 | 3.1 |  | 9.9 | 2.2 |  | 2.2 |  | 3.2 | 2.5 | 14.0 | 6.2 | 2.2 |  | 2.2 |  | 3.2 | 2.8 | 7.4 | 3.5 |
| 155 | 1.5 | 2.7 |  | 2.7 |  | 12.8 |  |  |  | 3.0 | 2.5 | 3.2 | 2.5 | 6.6 | 3.6 |  | 11.1 | 2.2 | 2.5 | 2.2 | 2.5 | 5.4 | 2.8 | 16.0 | 7.6 | 2.2 |  | 2.2 |  | 3.7 | 2.8 | 7.9 | 4.1 |
| 185 | 1.8 | 4.8 |  | 4.8 |  |  |  |  |  | 3.0 | 2.5 | 3.2 | 2.5 | 8.8 | 6.5 |  | 14.8 | 2.7 | 2.5 | 2.7 | 2.5 | 5.9 | 3.0 |  | 8.0 | 2.2 |  | 2.2 |  | 4.2 | 2.8 | 8.8 | 5.8 |
| 225 | 2.2 | 4.8 |  | 4.8 |  |  |  |  |  | 3.0 | 2.5 | 3.2 | 2.5 | 10.8 | 5.9 |  |  | 2.7 | 2.5 | 2.7 | 2.5 | 6.4 | 3.4 |  | 10.8 | 2.7 | 2.8 | 2.7 | 2.8 | 4.2 | 2.8 | 9.2 | 6.4 |
| 275 | 2.7 | 5.4 |  | 5.4 |  |  |  |  |  | 3.5 | 2.6 | 3.5 | 2.6 | 14.0 | 6.5 |  |  | 3.0 | 2.5 | 3.0 | 2.5 | 6.4 | 3.8 |  | 14.4 | 2.7 | 2.8 | 2.7 | 2.8 | 6.9 | 2.8 | 14.2 | 7.6 |
| 335 | 3.3 | 5.4 |  | 5.4 |  |  |  |  |  | 4 | 2.7 | 4 | 2.7 | 15 | 9.3 |  |  | 3 | 2.5 | 3 | 2.5 | 9.6 | 5.8 |  | 16 | 3.2 | 2.8 | 3.2 | 2.8 | 7.4 | 3.5 | 14 | 9.9 |
| 395 | 3.9 | 8.1 |  | 8.1 |  |  |  |  |  | 6 | 3 | 6.2 | 3 |  | 10 |  |  | 3.5 | 2.5 | 3.5 | 2.5 | 9.6 | 6.4 |  |  | 3.2 | 2.8 | 3.2 | 2.8 | 9.6 | 3.9 | 18 | 10 |
| 475 | 4.7 | 8.1 |  | 8.1 |  |  |  |  |  | 6.0 | 3.3 | 6.4 | 3.3 |  | 12.4 |  |  | 3.7 | 2.5 | 3.7 | 2.5 | 12.8 | 7.2 |  |  | 3.2 | 2.8 | 3.2 | 2.8 | 11.2 | 5.6 |  | 13.4 |
| 565 | 5.6 | 10.8 |  | 10.8 |  |  |  |  |  | 7.0 | 5.2 | 7.2 | 5.2 |  | 13.6 |  |  | 6.0 | 2.8 | 6.0 | 2.8 | 16.0 | 7.6 |  |  | 3.7 | 2.8 | 3.7 | 2.8 | 12.6 | 6.3 |  | 15.8 |
| 685 | 6.8 | 12.8 |  | 12.8 |  |  |  |  |  | 8.0 | 5.4 | 8.2 | 5.4 |  |  |  |  | 6.0 | 3.2 | 6.0 | 3.2 |  | 10.6 |  |  | 3.7 | 2.8 | 3.7 | 2.8 | 13.0 | 7.4 |  |  |
| 825 | 8.2 |  |  |  |  |  |  |  |  | 11.0 | 6.0 | 11.2 | 6.0 |  |  |  |  | 7.2 | 3.8 | 9.0 | 3.8 |  | 11.4 |  |  | 3.7 | 2.8 | 3.9 | 2.8 | 16.8 | 8.4 |  |  |
| 106 | 10 |  |  |  |  |  |  |  |  | 12.0 | 8.1 | 12.2 | 8.1 |  |  |  |  | 7.4 | 5.0 | 9.0 | 5.0 |  | 14.8 |  |  | 6.4 | 3.0 | 6.6 | 3.0 |  | 10.5 |  |  |
| 126 | 12 |  |  |  |  |  |  |  |  | 14.0 | 9.0 | 14.4 | 9.0 |  |  |  |  | 10.5 | 5.6 | 12.0 | 5.6 |  |  |  |  | 7.4 | 3.4 | 7.6 | 3.4 |  | 13.3 |  |  |
| 156 | 15 |  |  |  |  |  |  |  |  |  | 12.0 |  | 12.0 |  |  |  |  | 11.1 | 7.8 | 12.5 | 7.8 |  |  |  |  | 10.1 | 5.6 | 10.3 | 5.6 |  | 15.6 |  |  |
| 186 | 18 |  |  |  |  |  |  |  |  |  | 13.2 |  | 13.2 |  |  |  |  | 14.8 | 8.8 | 15.0 | 8.8 |  |  |  |  | 12.8 | 5.8 | 13.0 | 5.8 |  |  |  |  |
| 226 | 22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 10.2 |  | 10.2 |  |  |  |  | 14.8 | 6.4 | 15.0 | 6.4 |  |  |  |  |
| 276 | 27 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 11.2 |  | 11.2 |  |  |  |  | 14.8 | 8.8 | 15.0 | 8.8 |  |  |  |  |
| 336 | 33 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 15.0 |  | 15.0 |  |  |  |  | 16 | 9.8 | 16 | 9.8 |  |  |  |  |
| 396 | 39 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 12 |  | 12 |  |  |  |  |
| 476 | 47 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 12.0 |  | 12.0 |  |  |  |  |
| 566 | 56 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 686 | 68 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 826 | 82 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 107 | 100 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

The thickness (Tmax in mm) for SC Series or the Height (Hmax in mm) for the SV Series is indicated in the cells.

| Cr | Cr | SC04/SV04 (5550) | SC05/SV05 (6560) | SC06/SC07 SV06/SV07 (6080/8060) | SC10 (45107) |
| --- | --- | --- | --- | --- | --- |
| Code | (µF) | 50V | 100V | 200V | 500V | 50V | 100V | 200V 250 V | 500V 400V | 50V | 100V | 200V | 500V | 50V | 100V | 200V | 500V |
| 104 | 0.10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 124 | 0.12 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 154 | 0.15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 184 | 0.18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 224 | 0.22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 274 | 0.27 |  |  |  |  |  |  | 2.7 | 2.8 |  |  |  |  |  |  | 2.2 | 2.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 334 | 0.33 |  |  |  |  |  |  | 2.7 | 2.8 |  |  |  |  |  |  | 2.2 | 2.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 394 | 0.39 |  |  |  |  |  |  | 2.7 | 2.8 |  |  |  |  |  |  | 2.2 | 2.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 474 | 0.47 |  |  |  |  |  |  | 3.2 | 2.8 |  |  |  |  |  |  | 2.2 | 2.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 564 | 0.56 |  |  |  |  |  |  | 3.2 | 2.8 |  |  |  |  | 2.2 |  | 2.2 | 2.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 684 | 0.68 |  |  |  |  |  |  | 3.2 | 2.8 |  |  |  |  | 2.2 |  | 2.7 | 2.8 |  |  |  |  |  |  | 3.2 | 2.8 |  |  |  |  |  |  | 2.7 |  |
| 824 | 0.82 |  |  |  |  | 3.2 |  | 5.9 | 2.8 |  |  |  |  | 2.2 |  | 3.2 | 2.8 |  |  |  |  |  |  | 3.2 | 2.8 |  |  |  |  | 2.2 |  | 3.2 |  |
| 105 | 1.0 |  |  |  |  | 3.2 |  | 6.4 | 3.0 | 2.2 |  | 2.2 |  | 2.2 | 2.8 | 3.2 | 2.8 |  |  |  |  |  |  | 3.2 | 2.8 | 2.2 |  | 2.2 |  | 2.2 |  | 3.2 |  |
| 125 | 1.2 |  |  |  |  | 3.2 | 2.8 | 6.4 | 3.5 | 2.2 |  | 2.2 |  | 2.2 | 2.8 | 3.7 | 2.8 |  |  |  |  |  |  | 3.7 | 2.8 | 2.2 |  | 2.2 |  | 2.2 |  | 3.7 |  |
| 155 | 1.5 |  |  |  |  | 3.2 | 2.8 | 9.6 | 3.8 | 2.2 |  | 2.2 |  | 2.7 | 2.8 | 4.2 | 3.2 |  |  |  |  | 3.2 |  | 4.2 | 2.8 | 2.2 |  | 2.2 |  | 2.7 |  | 6.4 |  |
| 185 | 1.8 | 2.7 |  | 2.7 |  | 3.2 | 2.8 | 9.6 | 4.3 | 2.2 |  | 2.2 |  | 2.7 | 2.8 | 5.2 | 3.2 |  |  |  |  | 3.2 |  | 6.4 | 2.8 | 2.2 |  | 2.2 |  | 2.7 |  | 6.4 |  |
| 225 | 2.2 | 2.7 |  | 2.7 |  | 5.9 | 2.8 | 9.6 | 6.5 | 2.2 |  | 2.2 |  | 2.7 | 2.8 | 6.9 | 3.5 |  |  |  |  | 3.2 | 2.8 | 6.9 | 2.8 | 2.2 |  | 2.2 |  | 2.7 |  | 6.4 |  |
| 275 | 2.7 | 2.7 |  | 2.7 |  | 6.4 | 2.8 | 12.8 | 7.3 | 2.2 | 2.8 | 2.2 | 2.8 | 3.2 | 2.8 | 7.9 | 4.0 |  |  |  |  | 3.2 | 2.8 | 9.6 | 3.5 | 2.2 |  | 2.2 |  | 3.2 |  | 7.4 |  |
| 335 | 3.3 | 2.7 | 2.8 | 2.7 | 2.8 | 6.4 | 3.0 | 14.8 | 8.1 | 2.2 | 2.8 | 2.2 | 2.8 | 3.2 | 2.8 | 8.4 | 4.5 |  |  |  |  | 3.2 | 2.8 | 10.1 | 4.1 | 2.2 |  | 2.2 |  | 3.2 |  | 9.6 |  |
| 395 | 3.9 | 2.7 | 2.8 | 2.7 | 2.8 | 6.4 | 3.3 | 16.8 | 11.1 | 2.2 | 2.8 | 2.2 | 2.8 | 3.7 | 2.8 | 11.1 | 6.7 | 3.2 |  | 3.2 |  | 6.4 | 2.8 | 12.8 | 4.6 | 2.2 |  | 2.2 |  | 5.4 |  | 12.8 |  |
| 475 | 4.7 | 3.2 | 2.8 | 3.2 | 2.8 | 9.6 | 3.7 |  | 11.4 | 2.2 | 2.8 | 2.2 | 2.8 | 5.4 | 2.8 | 12.6 | 7.5 | 3.2 |  | 3.2 |  | 6.4 | 2.8 | 14.8 | 6.3 | 2.2 |  | 2.2 |  | 5.9 |  | 14.8 |  |
| 565 | 5.6 | 3.2 | 2.8 | 3.2 | 2.8 | 9.6 | 5.6 |  | 14.9 | 2.7 | 2.8 | 2.7 | 2.8 | 5.9 | 3.1 | 16.8 | 8.5 | 3.2 |  | 3.2 |  | 6.4 | 2.8 | 14.8 | 7.0 | 2.7 |  | 2.7 |  | 6.4 |  | 14.8 |  |
| 685 | 6.8 | 3.2 | 2.8 | 3.2 | 2.8 | 11.0 | 6.0 |  | 16.7 | 2.7 | 2.8 | 2.7 | 2.8 | 6.4 | 3.5 | 20.8 | 9.0 | 3.2 | 2.8 | 3.2 | 2.8 | 6.4 | 3.2 | 16.8 | 8.1 | 2.7 |  | 2.7 |  | 8.1 |  | 16.8 |  |
| 825 | 8.2 | 3.7 | 2.8 | 3.7 | 2.8 | 11.1 | 6.4 |  |  | 3.2 | 2.8 | 3.2 | 2.8 | 9.1 | 4.0 |  | 12.0 | 3.2 | 2.8 | 3.2 | 2.8 | 9.6 | 3.8 |  | 9.8 | 3.2 |  | 3.2 |  | 9.6 |  |  |  |
| 106 | 10 | 4.0 | 2.8 | 5.4 | 2.8 | 12.6 | 9.4 |  |  | 3.2 | 2.8 | 3.2 | 2.8 | 9.6 | 5.9 |  | 13.5 | 3.7 | 2.8 | 3.7 | 2.8 | 9.6 | 5.6 |  | 12.3 | 3.2 |  | 3.2 |  | 9.6 |  |  |  |
| 126 | 12 | 6.4 | 3.0 | 6.4 | 3.0 | 16.0 | 9.9 |  |  | 3.7 | 2.8 | 5.4 | 2.8 | 12.8 | 6.6 |  | 17.5 | 3.7 | 2.8 | 3.7 | 2.8 | 12.8 | 6.0 |  | 15.1 | 3.7 |  | 3.7 |  | 12.8 |  |  |  |
| 156 | 15 | 7.2 | 3.4 | 8.1 | 3.4 |  | 13.2 |  |  | 4.2 | 2.8 | 5.9 | 2.8 | 14.8 | 7.5 |  |  | 3.7 | 2.8 | 3.7 | 2.8 | 12.8 | 7.0 |  | 18.4 | 6.4 |  | 6.4 |  | 12.8 |  |  |  |
| 186 | 18 | 7.7 | 5.6 | 10.8 | 5.6 |  | 14.4 |  |  | 6.4 | 2.8 | 6.4 | 2.8 |  | 10.1 |  |  | 3.7 | 2.8 | 3.7 | 2.8 | 16.0 | 8.8 |  |  | 6.4 |  | 6.4 |  | 16.8 |  |  |  |
| 226 | 22 | 8.0 | 5.8 | 12.8 | 5.8 |  |  |  |  | 6.4 | 3.2 | 6.4 | 3.2 |  | 11.0 |  |  | 6.4 | 3.0 | 7.4 | 3.0 |  | 9.2 |  |  | 9.6 |  | 9.6 |  |  |  |  |  |
| 276 | 27 | 11.7 | 6.2 | 12.8 | 6.2 |  |  |  |  | 7.9 | 3.8 | 9.6 | 3.8 |  | 14.0 |  |  | 6.4 | 3.5 | 8.2 | 3.5 |  | 12.8 |  |  | 9.6 |  | 9.6 |  |  |  |  |  |
| 336 | 33 | 12.0 | 8.6 | 14.8 | 8.6 |  |  |  |  | 8.4 | 5.6 | 9.6 | 5.6 |  | 16.0 |  |  | 7.1 | 5.6 | 10.5 | 5.6 |  | 15.2 |  |  | 12.8 |  | 12.8 |  |  |  |  |  |
| 396 | 39 | 16.0 | 9.4 | 16.8 | 9.4 |  |  |  |  | 11.6 | 6.0 | 12.8 | 6.0 |  |  |  |  | 9.6 | 5.8 | 11.2 | 5.8 |  |  |  |  | 12.8 |  | 12.8 |  |  |  |  |  |
| 476 | 47 |  | 12.0 |  | 12.0 |  |  |  |  | 12.6 | 7.0 | 12.8 | 7.0 |  |  |  |  | 9.6 | 6.5 | 11.8 | 6.5 |  |  |  |  | 16.0 |  | 16.0 |  |  |  |  |  |
| 566 | 56 |  | 13.6 |  | 13.6 |  |  |  |  | 16.8 | 8.8 | 17.0 | 8.8 |  |  |  |  | 11.6 | 8.8 | 12.0 | 8.8 |  |  |  |  |  |  |  |  |  |  |  |  |
| 686 | 68 |  |  |  |  |  |  |  |  |  | 9.6 |  | 9.6 |  |  |  |  | 14.8 | 9.0 | 15.0 | 9.0 |  |  |  |  |  |  |  |  |  |  |  |  |
| 826 | 82 |  |  |  |  |  |  |  |  |  | 12.8 |  | 12.8 |  |  |  |  |  | 11.8 |  | 11.8 |  |  |  |  |  |  |  |  |  |  |  |  |
| 107 | 100 |  |  |  |  |  |  |  |  |  | 14.6 |  | 14.6 |  |  |  |  |  | 13.5 |  | 13.5 |  |  |  |  |  |  |  |  |  |  |  |  |

The thickness (Tmax in mm) for SC Series or the Height (Hmax in mm) for the SV Series is indicated in the cells.

VI-3 Dimensions

SC Series

4 wires « W4 » terminations	All dimensions in mm

| Size | L | W | LS | p |  | H |
| --- | --- | --- | --- | --- | --- | --- |
|  | max | max | ± 0,5 | ± 0,5 | ± 10% | max |
| SC02 | 11,9 | 11,4 | 10,20 | 7,62 | 0,6 | Please, consult the tables of capacitance range |
| SC03 | 17,0 | 12,0 | 15,24 | 10,16 | 0,9 |  |
| SC04 | 16,5 | 14,0 | 15,24 | 10,16 | 0,9 |  |
| SC05 | 20,0 | 16,6 | 17,80 | 10,16 | 0,9 |  |
| SC06 | 17,8 | 21,6 | 15,24 | 10,16 | 0,9 |  |
| SC07 | 22,7 | 16,6 | 20,32 | 10,16 | 0,9 |  |

Dual In Line « DIL » termination	All dimensions in mm

| Size | L | W | LS | E | D | Nb | H |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | max | max | ± 0,5* | ± 0,3 | ± 0,5 | pins** | max |
| SC00 | 7,4 | 8,5 | 6,35 | 2,0 | 2,0 | 3 | Please, consult the tables of capacitance range |
| SC01 | 10,2 | 9,6 | 7,62 | 1,5 | 2,5 | 3 |  |
| SC02 | 11,9 | 11,4 | 10,16 | 1,5 | 2,5 | 4 |  |
| SC03 | 15,5 | 11,5 | 14,00 | 1,5 | 2,5 | 4 |  |
| SC04 | 16,5 | 14,0 | 13,70 | 1,5 | 2,5 | 5 |  |
| SC05 | 18,5 | 17,0 | 17,78 | 1,5 | 2,5 | 6 |  |
| SC06 | 17,8 | 21,6 | 15,24 | 1,5 | 2,5 | 7 |  |
| SC07 | 22,7 | 16,6 | 20,32 | 1,5 | 2,5 | 6 |  |
| SC10 | 13,2 | 27,5 | 11,50 | 2,1 | 2,6 | 10 |  |

* Except for the SC07, tolerance = ± 0.8 mm

* * Number de pins per side

Wires bending: 10° max

Note: the marking shown here is just given as an example

.

Ribbons “R” terminations

All dimensions in mm

| Size | L | W | A | H |
| --- | --- | --- | --- | --- |
|  | max | max | ± 0,2 | max |
| SC01 | 10,2 | 9,6 | 8,0 | Please, consult the tables of capacitance range |
| SC02 | 11,9 | 11,4 | 8,0 |  |
| SC03 | 15,5 | 11,5 | 8,0 |  |
| SC04 | 16,5 | 14,0 | 8,0 |  |
| SC05 | 18,5 | 17,0 | 15,0 |  |
| SC06 | 17,8 | 21,6 | 15,0 |  |
| SC07 | 22,7 | 16,6 | 15,0 |  |

Note: the marking shown here is just given as an example

SV Series

All dimensions in mm

| Size | W max | H max | LS ±0.5 |  ±10% | T max |
| --- | --- | --- | --- | --- | --- |
| SV01 | 10,2 | 9,6 | 10,16 | 0,6 | Please, consult the tables of capacitance range |
| SV02 | 11,9 | 11,4 | 10,16 | 0,6 |  |
| SV03 | 17,0 | 12,0 | 15,24 | 0,9 |  |
| SV04 | 16,5 | 14,0 | 15,24 | 0,9 |  |
| SV05 | 20,0 | 16,6 | 17,80 | 0,9 |  |
| SV06 | 17,8 | 21,6 | 15,24 | 0,9 |  |
| SV07 | 22,7 | 16,6 | 20,32 | 0,9 |  |

VI-4 Marking

| Size | Marking codes | Example |
| --- | --- | --- |
| All sizes | « TA » logo Cap Code + Tolerance Code Rated voltage value |  |

# VII “TB” Series

VII-1 Features

This series features have the same electrical parameters than the “SC” series with only 4 wires variants, the capacitor being molded in a plastic housing making it perfectly impervious to all external agents.

VII-2 Capacitance range and dimensions

| Cr | Cr | TB Series |
| --- | --- | --- |
| Code | (µF) | 63V | 100V | 250V | 400V |
| 684 | 0.68 |  |  | TB01 | TB01 |
| 824 | 0.82 |  |  | TB01 | TB01 |
| 105 | 1.0 |  |  | TB01 | TB01 |
| 125 | 1.2 |  |  | TB01 | TB01 |
| 155 | 1.5 |  |  | TB01 | TB02 |
| 185 | 1.8 |  |  | TB01 | TB02 |
| 225 | 2.2 |  | TB01 | TB01 | TB03 |
| 275 | 2.7 |  | TB01 | TB01 | TB03 |
| 335 | 3.3 |  | TB01 | TB01 | TB03 |
| 395 | 3.9 |  | TB01 | TB02 | TB03 |
| 475 | 4.7 |  | TB01 | TB02 | TB03 |
| 565 | 5.6 | TB01 | TB01 | TB02 | TB04 |
| 685 | 6.8 | TB01 | TB01 | TB02 | TB04 |
| 825 | 8.2 | TB01 | TB01 | TB03 |  |
| 106 | 10 | TB01 | TB01 | TB03 |  |
| 126 | 12 | TB01 | TB01 | TB03 |  |
| 156 | 15 | TB01 | TB01 |  |  |
| 186 | 18 | TB02 | TB02 |  |  |
| 226 | 22 | TB03 | TB03 |  |  |
| 276 | 27 | TB03 | TB03 |  |  |
| 336 | 33 | TB03 | TB03 |  |  |
| 396 | 39 | TB03 | TB03 |  |  |
| 476 | 47 | TB03 | TB03 |  |  |
| 566 | 56 | TB04 | TB04 |  |  |
| 686 | 68 | TB04 |  |  |  |
| 826 | 82 | TB04 |  |  |  |
| 107 | 100 | TB05 |  |  |  |

VII-3 Marking

| Size | Marking codes | Example |
| --- | --- | --- |
| All sizes | « TA » logo Cap Code + Tolerance Code Rated voltage value |  |

The marking is applied on the top of the TB capacitors

# VII Dielectric characteristics

| Description | “X” Series (class 2) | “T” Series (class 2) |
| --- | --- | --- |
| CECC | 2R1 | 2R1 |
| EIA | X7R | X7R |
| Temex Ceramics Code | X | T |
| Operating temperature range | -55°C / +125°C | -55°C / +125°C |
| Storage temperature range | -55°C / +125°C | -55°C / +125°C |
| Maximun C/C over Temperature range without voltage applied | ( 15% | ( 15% |
| Ageing | ≤2.5% per decade hour | ≤2.5% per decade hour |
| Dissipation Factor (D.F.) | ≤ 2.5% | ≤ 2.5% |
| Voltage proof | Ur ≤ 200V: 2.5 x Ur Ur > 200V: 2.0 x Ur | Ur ≤ 200V: 2.5 x Ur Ur > 200V: 2.0 x Ur |
| Insulation Resistance (IR) @ 25°C (Under Ur) | 100G( or 1000(.F* | 100G( or 1000(.F* |
| Insulation Resistance (IR) @ 125°C (Under Ur) | 10G( or 100(.F* | 10G( or 100(.F* |
| Measurement Conditions for C and D.F. @ 20°C | ≤ 100pF: 1MHz / 1Vrms (no bias) > 100pF: 1KHz / 1Vrms (no bias) | ≤ 100pF: 1MHz / 1Vrms (no bias) > 100pF: 1KHz / 1Vrms (no bias) |

(*): whichever is the less.

Curves of capacitance behaviour versus applied voltage @25°C (for all sizes)

Curves of capacitance behaviour versus temperature (for all sizes), without voltage

# V Electrical characteristics

# VII Termination types

| Description | P (RoHS) | T (non RoHS) | R / W2 / W4 (RoHS version) | R / W2 / W4 (non RoHS version) | DIL (RoHS version) | DIL (non RoHS version) |
| --- | --- | --- | --- | --- | --- | --- |
| Chip (SMD) | ( | ( | - | - | - | - |
| Leaded caps | - | - | ( | ( | ( | ( |
| Materials | All sizes: Pure Ag Or AgPd | P termination with SnPbAg solder dipping | 100% tinned Copper | Sn(70%) Pb(30%) plated Copper | 100% tinned phosphor bronze | Sn(60%) Pb(40%) plated phosphor bronze |
| Magnetic status | Non magnetic | Non magnetic | Non magnetic | Non magnetic | Non magnetic | Non magnetic |
| Lead status (% of Pb) | 0% | 36% | 0% | 30% of the plated layer | 0% | 40% of the plated layer |

# VIII Special products

As standard products can’t meet all the specificities of all applications, special applications may require special features (higher voltage, burn-in, dimensions, coating, leading, marking…) not described in this catalogue.

Based on the “state of the Art”, and our knowledge of the technology, our Engineers may study at your request all special components to meet your application.

Please, consult us for more information.

# IX How to order

(**): For leaded capacitors, both RoHS and non-RoHS versions exist. This is due to the wishes of some customers who still need non-RoHS components in their applications. This suffix must be required for RoHS compliancy.

For “P” terminations, only the RoHS version exists. The RoHS suffix can be added for information.

# X Packaging

“Blister” Boxes (SMD and leaded components):

For all products, special “blister” boxes are used to optimise the protection of the parts during the carriage and the storage. Depending upon the termination (with or without connection) and the size, the number of the parts in each box is defined. Please, consult us for more details.

# Text boxes

Termination

W4

Size

01

02

03

04

05

Family

TB

Size

00 (SC only)

01

02

03

04

05

06

07

10 (SC only)

Family

SC

SV

Coating

(not available for chips and TB caps)

If left blank

Uncoated and

No marking

U

Uncoated and marked

C

Coated and marked

Termination

SC Series

DN

DJ

DL

RL

RJ

W4

SV Series

W2

Termination

P

T

R

RoHS

Compliancy

(**)

If left blank

non-RoHS compliant

Tolerance

K ((10%)

M ((20%)

Capacitance

1st two digits are significant; third digit denotes number of zeros

Exemples:

101=100pF

472= 4.7nF

683 = 68nF

104 = 0.1µF

Size

2229

3033

3740

5440

5550

6560

6080

8060

45107

Family

R

CNC

Dielectric

N = NP0

X = X7R

T = X7R

Rated

Voltage

1st two digits are significant; third digit denotes number of zeros

Exemples:

201= 200V

501 = 500V

-RoHS

P

K

( D

T

25mm

mini

H

W

“X” series in green cells	“T” series in blue cells

W

105

T

EB

L

EB

“X” series in green cells	“T” series in blue cells

B

T

These typical curves are an example of admissible currents for one family of chip capacitors. For other curves and products or for further information, please contact us.

Note: for the calculations, we have considered that the terminations are directly connected to an infinite heat sink.  In other words, the thermal resistance of the circuit itself which depends of its type and design has not been taken into account. Moreover, the ambient temperature taken is 25°C.

L

B

X

LS

2.5mm

maxi

EB

EB

W

( D

T

25mm

mini

H

W

LS

2.5mm

maxi

“X” series in green cells

“X” series in green cells	“T” series in blue cells

“X” series in green cells	“T” series in blue cells

“X” series in green cells	“T” series in blue cells

“X” series in green cells	“T” series in blue cells

L

H



25

min

LS

TA

105M

100V

W

p

L

H

3.75

min

LS ± 0.5

“N” Type

“J” Type

“L” Type

E

D

H

L

LS ± 0.5

E

H

L

LS ± 0.5

D

W

0.5

2.54

W

2.54

0.5

W

0.5

2.54

TA

105M

100V

0.25

TA

105M

100V

0.25

0.25

TA

105M

100V

1.5± 0.3

2.5 ± 0.5

H

L

0.3 ± 0.05

Z ±0.5

10° max

2.5 ± 0.5

H

L

Z ±0.5

0.3 ± 0.05

A

TA

105M

100V

W

A

TA

105M

100V

W

1.5± 0.3

0.9

H

19±1

10.16 ± 0.5

21±1

17.8 ± 0.8

15

min

“X” series in green cells

The ESR (Equivalent Serial Resistance) curves are given here for SMD (chips) capacitors. Regarding the curves for the leaded capacitors, they are rather the same.

Indeed, due to the resistivity of the raw material used and the wire diameters, the resistance of the wires is much lower than the ESR of the chips. So, in a first approach, their influence can be considered as negligible.

6560

R

501

TA

105M

100V

105M

100V

TA

105M

100V



TA

105M

100V

LS

25

min

W

T

H

TA

105M

100V

TA

105M

100V

TA

105M

100V

TA

105M

100V