#### TABLE OF CONTENTS

I. 	General description	3

II 	Case sizes and dimensions	3

III 	Capacitance ranges	4

IV 	Dielectric characteristics	6

V 	Electrical characteristics	7

VII 	How to order	8

XI 	Packaging	9

# I. General description

This family of SMD products has been developed with four dielectrics to answer to the high capacitance values demands in a very small case sizes. These capacitors perfectly suit to high reliability applications and have excellent performances on radio frequencies. The main applications concern the smoothing, decoupling circuits, generally for DC-DC converters, personal computers and general electronic equipments.

This family is RoHS compliant.

# II Case sizes and dimensions

All dimensions in mm.

| Sizes | L | W | T (max) | B (min) | BW (min) |
| --- | --- | --- | --- | --- | --- |
| R07 = 0402 | 1.00±0.05 | 0.50±0.05 | 0.55 | 0.3 | 0.15 |
| R14 = 0603 | 1.60±0.10 | 0.80±0.10 | 0.90 | 0.4 | 0.15 |
| R15 = 0805 | 2.00±0.20 | 1.25±0.20 | 1.45 | 0.7 | 0.2 |
| R18 = 1206 | 3.20±0.30 | 1.60±0.20 | 1.80 | 1.5 | 0.3 |
| S41 = 1210 | 3.20±0.30 | 2.50±0.20 | 2.60 | 1.6 | 0.3 |
| S43 = 1812 | 4.60±0.30 | 3.20±0.30 | 3.00 | 2.5 | 0.3 |
| S47 = 2220 | 5.70±0.40 | 5.00±0.40 | 3.00 | 3.5 | 0.3 |

# III Capacitance ranges

|  |  | NP0 (N Series) |
| --- | --- | --- |
| Cr | Cr | R14 | R15 | R18 | S41 | S43 |
| Code | (nF) | 16V | 25V | 50V | 16V | 25V | 50V | 16V | 25V | 50V | 16V | 25V | 50V | 16V | 25V | 50V |
| 102 | 1.0 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 122 | 1.2 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 152 | 1.5 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 182 | 1.8 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 222 | 2.2 | 0.95 | 0.95 | 0.95 | 1.10 | 1.10 | 1.10 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 272 | 2.7 | 0.95 | 0.95 | 0.95 | 1.40 | 1.40 | 1.40 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 332 | 3.3 | 0.95 | 0.95 | 0.95 | 1.40 | 1.40 | 1.40 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 392 | 3.9 |  |  |  | 1.40 | 1.40 | 1.40 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 472 | 4.7 |  |  |  | 1.40 | 1.40 | 1.40 | 0.95 | 0.95 | 0.95 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 562 | 5.6 |  |  |  | 1.40 | 1.40 | 1.40 | 1.10 | 1.10 | 1.10 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 682 | 6.8 |  |  |  | 1.40 | 1.40 | 1.40 | 1.40 | 1.40 | 1.40 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 822 | 8.2 |  |  |  | 1.40 | 1.40 | 1.40 | 1.40 | 1.40 | 1.40 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 103 | 10 |  |  |  | 1.40 | 1.40 | 1.40 | 1.40 | 1.40 | 1.40 |  | 1.10 | 1.10 |  | 1.40 | 1.40 |
| 123 | 12 |  |  |  | 1.40 | 1.40 |  | 1.1/1.4 | 1.1/1.4 | 1.1/1.4 |  | 1.40 | 1.40 |  | 1.40 | 1.40 |
| 153 | 15 |  |  |  | 1.40 | 1.40 |  | 1.1/1.4 | 1.1/1.4 | 1.1/1.4 |  | 1.80 | 1.80 |  | 1.40 | 1.40 |
| 183 | 18 |  |  |  | 1.40 |  |  | 1.40 | 1.40 | 1.40 |  | 1.80 | 1.80 |  | 1.40 | 1.40 |
| 223 | 22 |  |  |  | 1.40 |  |  | 1.40 | 1.40 | 1.40 |  | 2.20 | 2.20 |  | 1.80 | 1.80 |
| 273 | 27 |  |  |  | 1.40 |  |  | 1.80 | 1.80 | 1.80 | 1.40 | 2.20 | 2.20 |  | 1.80 | 1.80 |
| 333 | 33 |  |  |  |  |  |  | 1.80 | 1.80 | 1.80 | 1.80 | 2.20 | 2.20 |  | 1.80 | 1.80 |
| 393 | 39 |  |  |  |  |  |  | 1.80 | 1.80 |  | 1.80 | 2.20 | 2.20 |  | 1.80 | 1.80 |
| 473 | 47 |  |  |  |  |  |  | 1.80 | 1.80 |  | 1.80 | 2.20 | 2.20 |  | 2.20 | 2.20 |
| 563 | 56 |  |  |  |  |  |  | 1.80 |  |  | 1.80 | 2.20 |  | 2.20 | 2.20 | 2.20 |
| 683 | 83 |  |  |  |  |  |  | 1.80 |  |  | 1.80 | 2.20 |  | 2.20 | 2.20 | 2.20 |
| 823 | 82 |  |  |  |  |  |  |  |  |  | 2.20 |  |  | 2.20 | 2.20 | 2.20 |
| 104 | 100 |  |  |  |  |  |  |  |  |  | 2.20 |  |  | 2.20 | 2.20 | 2.20 |
| 124 | 120 |  |  |  |  |  |  |  |  |  |  |  |  | 2.20 | 2.20 |  |
| 154 | 150 |  |  |  |  |  |  |  |  |  |  |  |  | 2.20 |  |  |
| 224 | 220 |  |  |  |  |  |  |  |  |  |  |  |  | 2.20 |  |  |

|  |  | X7R (X Series) |
| --- | --- | --- |
| Cr | Cr | R14 | R15 | R18 | S41 | S43 | S47 |
| Code | (µF) | 6.3V | 10V | 16V | 6.3V | 10V | 16V | 25V | 10V | 16V | 25V | 35V | 50V | 10V | 16V | 25V | 35V | 50V | 100V | 35V | 50V | 100V | 35V | 50V | 100V |
| 104 | 0.10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.10 | 1.10 |  | 1.40 | 1.4/1.8 |  |  |  |
| 154 | 0.15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.10 | 1.10 |  | 1.40 | 1.4/1.8 |  |  |  |
| 224 | 0.22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.10 | 1.10 |  | 1.40 | 1.4/1.8 |  |  |  |
| 334 | 0.33 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.10 | 1.10 |  | 1.40 | 1.4/1.8 |  |  |  |
| 474 | 0.47 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.40 | 1.10 |  | 1.40 | 1.80 |  | 1.80 | 1.80 |
| 564 | 0.56 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.40 | 1.40 |  | 1.40 | 1.80 |  | 1.80 | 1.80 |
| 684 | 0.68 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.40 | 1.80 |  | 1.40 | 1.80 |  | 1.80 | 1.80 |
| 105 | 1.0 | 0.95 | 0.95 | 0.95 |  | 1.40 | 1.40 | 1.40 |  | 1.80 | 1.80 | 1.80 | 1.80 |  | 1.80 | 1.80 | 1.80 | 1.80 | 2.20 | 2.20 | 1.40 | 1.80 | 2.20 | 2.20 | 2.20 |
| 155 | 1.5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.20 | 2.60 | 2.20 | 1.80 | 2.20 | 2.20 | 2.20 | 2.20 |
| 225 | 2.2 | 0.95 | 0.95 | 0.95 | 1.40 | 1.40 | 1.40 |  | 1.80 | 1.80 | 1.80 |  |  |  | 1.80 | 1.8/2.2 | 2.20 | 2.60 | 2.60 | 2.20 | 2.20 | 2.20 | 2.20 | 2.20 | 2.20 |
| 335 | 3.3 |  |  |  | 1.40 | 1.40 |  |  | 1.80 | 1.80 |  |  |  |  |  |  |  |  |  |  | 2.20 |  | 2.20 | 2.20 | 2.20 |
| 475 | 4.7 |  |  |  | 1.40 | 1.40 |  |  | 1.80 | 1.80 |  |  |  |  | 1.80 | 2.20 | 2.20 |  |  |  | 2.20 |  | 2.20 | 2.20 | 2.20 |
| 685 | 6.8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.60 |  |
| 106 | 10 |  |  |  |  |  |  |  | 1.80 |  |  |  |  | 1.80 | 1.80 | 2.20 | 2.60 |  |  |  |  |  | 2.60 | 3.00 |  |

|  |  | X5R (B Series) |
| --- | --- | --- |
| Cr | Cr | R07 | R14 | R15 | R18 | S41 |
| Code | (µF) | 6.3V | 10V | 4V | 6.3V | 10V | 16V | 25V | 4V | 6.3V | 10V | 16V | 25V | 6.3V | 10V | 16V | 25V | 35V | 50V | 6.3V | 10V | 16V | 25V | 35V |
| 105 | 1.0 | 0.55 | 0.55 |  | 0.95 | 0.95 | 0.95 | 0.95 |  |  | 1.40 | 1.40 | 1.40 |  |  | 1.80 | 1.80 | 1.80 | 1.80 |  |  |  |  | 2.20 |
| 155 | 1.5 |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.80 |  |  |  |  |  |  |  |  |  |
| 225 | 2.2 | 0.55 |  |  | 0.95 | 0.95 | 0.95 |  |  | 1.40 | 1.40 | 1.40 | 1.40 |  | 1.80 | 1.80 | 1.80 |  |  |  |  | 1.80 | 1.8/2.2 | 2.20 |
| 335 | 3.3 |  |  |  |  |  |  |  |  | 1.40 | 1.40 | 1.40 | 1.40 |  | 1.80 | 1.80 | 1.80 |  |  |  |  |  |  |  |
| 475 | 4.7 |  |  |  | 0.95 | 0.95 |  |  |  | 1.40 | 1.40 | 1.40 | 1.40 | 1.80 | 1.80 | 1.80 | 1.80 |  |  |  | 2.20 | 2.20 | 2.20 | 2.20 |
| 106 | 10 |  |  | 0.95 | 0.95 |  |  |  |  | 1.40 | 1.40 | 1.40 |  | 1.80 | 1.80 | 1.80 | 1.80 |  |  |  | 2.20 | 2.20 | 2.60 | 2.60 |
| 226 | 22 |  |  |  |  |  |  |  | 1.40 | 1.40 |  |  |  | 1.80 | 1.80 | 1.80 |  |  |  | 2.60 | 2.60 | 2.60 | 2.60 |  |
| 476 | 47 |  |  |  |  |  |  |  |  |  |  |  |  | 1.80 | 1.80 |  |  |  |  | 2.60 | 2.60 |  |  |  |
| 107 | 100 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.60 |  |  |  |  |

|  |  | X6S (U Series) |
| --- | --- | --- |
| Cr | Cr | R14 | R15 | R18 | S41 |
| Code | (µF) | 10V | 25V | 10V | 16V | 25V | 10V | 25V | 35V | 50V | 10V | 16V | 25V | 50V |
| 105 | 1.0 |  | 0.95 |  |  | 1.40 |  |  | 1.80 | 1.80 |  |  |  | 2.20 |
| 225 | 2.2 |  |  | 1.40 | 1.40 | 1.40 |  |  |  |  |  |  | 2.20 |  |
| 475 | 4.7 |  |  |  | 1.40 | 1.40 | 1.80 | 1.80 |  |  |  | 2.20 | 2.20 |  |
| 106 | 10 | 0.95 |  | 1.40 |  |  | 1.80 | 1.80 |  |  | 2.20 | 2.20 | 2.60 |  |
| 226 | 22 |  |  |  |  |  |  |  |  |  | 2.60 | 2.60 | 2.60 |  |
| 476 | 47 |  |  |  |  |  |  |  |  |  |  |  |  |  |

|  |  | Y5V (Y Series) |
| --- | --- | --- |
| Cr | Cr | R07 | R14 | R15 | R18 | S41 | S43 |
| Code | (µF) | 6.3V | 10V | 6.3V | 10V | 16V | 25V | 6.3V | 10V | 16V | 25V | 50V | 10V | 16V | 25V | 35V | 50V | 6.3V | 10V | 16V | 25V | 35V | 50V | 35V | 50V |
| 105 | 1.0 | 0.55 | 0.55 |  | 0.95 | 0.95 | 0.95 |  |  | 0.95 | 0.95 | 1.40 |  | 0.95 | 1.40 | 1.40 | 1.40 |  |  |  |  |  |  |  |  |
| 225 | 2.2 |  |  | 0.95 | 0.95 | 0.95 |  |  | 1.40 | 1.40 | 1.40 |  |  | 0.95 | 1.40 | 1.40 |  |  |  |  |  |  |  |  |  |
| 475 | 4.7 |  |  | 0.95 | 0.95 |  |  | 1.40 | 1.40 | 1.40 |  |  |  | 1.40 | 1.40 |  |  |  |  |  | 2.20 | 2.20 | 2.20 |  | 2.20 |
| 106 | 10 |  |  |  |  |  |  | 1.40 | 1.40 | 1.40 |  |  | 1.40 | 1.80 | 1.80 |  |  |  |  | 2.20 | 2.20 | 2.20 | 2.20 | 2.20 | 2.20 |
| 226 | 22 |  |  |  |  |  |  | 1.40 |  |  |  |  | 1.40 | 1.80 |  |  |  |  | 2.20 | 2.20 | 2.20 |  |  | 2.20 |  |
| 476 | 47 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.20 | 2.20 |  |  |  |  |  |  |
| 107 | 100 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 2.60 |  |  |  |  |  |  |  |

# IV Dielectric characteristics

| Designation | NP0 | X7R | X5R | X6S | Y5V |
| --- | --- | --- | --- | --- | --- |
| Temex Ceramics Series | N | X | B | U | Y |
| EIA Class | Class I | Class II | Class II | Class II | Class II |
| Temperature range | -55°C to +125°C | -55°C to +125°C | -55°C to +85°C | -55°C to +105°C | -55°C to +85°C |
| Temperature coefficient | ≤ 30ppm/°C | NA | NA | NA | NA |
| Maximun C/C over Temperature range without voltage applied | NA | ± 15% | ± 15% | ± 22% | +22/-82% |
| Capacitance range | 1 to 220nF | 1 to 10uF | 1 to 100uF | 1 to 22uF | 1 to 47uF |
| Voltage proof | 250% rated voltage | 250% rated voltage | 250% rated voltage | 250% rated voltage | 250% rated voltage |
| Insulation resistance | 10G( or 500(F * > 100(F ** | 10G( or 500(F * > 100(F ** | 10G( or 500(F * > 100(F ** | 10G( or 500(F * > 100(F ** | 10G( or 500(F * > 100(F ** |
| Aging | None | ≤ 2.5% (per decade hour) | ≤ 2.5% (per decade hour) | ≤ 2.5% (per decade hour) | ≤ 7.0% (per decade hour) |

(*): whichever is the less, for Ur > 10 volts

(**): greater than, for Ur ≤ 10 volts

# V Electrical characteristics

# VII How to order

# XI Packaging

Tape and reel

| Sizes | Thickness (mm) | Paper Tape (parts/reel) | Plastic Tape (parts/reel) |
| --- | --- | --- | --- |
| R07 = 0402 | T ≤ 0.55 | 10000 | - |
| R14 = 0603 | T ≤ 0.90 | 4000 | - |
| R15 = 0805 | T ≤ 0.90 0.90 ≤ T ≤ 1.25 | 4000 - | - 3000 |
| R18 = 1206 | T ≤ 0.90 0.90 ≤ T ≤ 1.25 T > 1.25 | 4000 - - | - 3000 2000 |
| S41 = 1210 | T ≤ 1.25 T > 1.25 | - - | 3000 2000 |
| S43 = 1812 | T ≤ 2.20 T > 2.20 | - - | 1000 700 |
| S47 = 2220 | T ≤ 2.20 T > 2.20 | - - | 1000 700 |

Diameter of the reels: 180mm.

# Text boxes

Packaging

E

(tape & reel)

The NPO products can be use for the replacement of film capacitors. Here is a caparison of the temperature coefficients.

The maximum thickness is indicated in the tables

E

Termination

S

(Nickel barrier covered by 100% Matte tin plating)

Tolerance

Class1 diel.

F ((1%)

G ((2%)

J ((5%)

Class2 diel.

K ((10%)

M ((20%)

Capacitance

1st two digits are significant; third digit denotes number of zeros

Exemples:

101=100pF

472= 4.7nF

683 = 68nF

104 = 0.1µF

Family

R07=0402

R14=0603

R15=0805

R18=1206

S41=1210

S43=1812

S47=2220

Dielectric

N = NP0

X = X7R

B = X5R

U = X6S

Y = Y5V

Rated

Voltage

<10V

The voltage value is got by dividing by 10 the voltage code

≥ 10V

1st two digits are significant; third digit denotes number of zeros

Exemples:

040=4.0V

063=6.3V

100=10V

160=16V

250=25V

350=35V

500=50V

S

K

106

X

S41

350